# Example 4 - Plackett-Burman Design

Download Example File for Version 10 (*.rsgz10) or Version 9 (*.rsr9)

## Background

The Plackett-Burman design type is one of the so-called "screening designs." Such designs are traditionally used for identifying important factors from among many potential factors. In the analysis of these designs, usually only main effects are estimated.

Consider a life test of weld-repaired castings.* The objective of the test is to identify the factors that affect the life of the product, and then determine the settings that will improve the life. There are seven potentially significant factors. A two level full factorial design would require 27 = 128 runs, and thus would be time-consuming and costly. Therefore, a Plackett-Burman experiment consisting of eight runs will be conducted.

For this example, the seven factors are:

| Name | Low Level | High Level |
| --- | --- | --- |
| Initial Structure | As Received | Beta Treat |
| Bead Size | Small | Large |
| Pressure Treat | None | HIP |
| Heat Treat | Anneal | Solution Treat/Age |
| Cooling Rate | Slow | Rapid |
| Polish | Chemical | Mechanical |
| Final Treat | None | Peen |

The recorded response is the logarithmically transformed failure time for each test unit.

## Experiment Design

To find the important factors, the experimenters use the standard design folio in DOE++ to create a Plackett-Burman factorial design. On the Design tab of the folio, the following design settings are specified. The design matrix and response data are given on the Data tab of the "Cast Fatigue Experiment" folio.

## Analysis

Step 1: When the design is built, the experiment runs are shown in a randomized order on the Data tab. After performing the runs in the displayed order and recording the results, the experimenters enter the data set into the folio, as shown next.

Figure 1: The data set entered on the Data tab of the folio.

Step 2: Next, the analysis settings are specified. The data set will be analyzed using the default risk (significance) level of 0.1. In addition, the test statistic for the effects will be calculated using the partial sum of squares, and the ANOVA table will show the results for each individual term.

Figure 2: Analysis settings.

Step 3: An effect probability plot is created, as shown next. The plot shows that effect F is significant.

Figure 3: Effect probability plot indicating the significant effect.

## Conclusions

The effects of all the factors are shown in the Regression Information table in the detailed summary of results:

| Regression Information |  |  |
| --- | --- | --- |
| Term | Effect | Coefficient |
| Intercept |  | 5.904 |
| A:Initial Structure | -0.142 | -0.071 |
| B:Bead Size | -0.082 | -0.041 |
| C:Pressure Treat | -0.368 | -0.184 |
| D:Heat Treat | -0.002 | -0.001 |
| E:Cooling Rate | -0.128 | -0.064 |
| F:Polish | 2.232 | 1.116 |
| G:Final Treat | 0.258 | 0.129 |

As indicated by the positive/negative effect values, assuming that there is no interaction, a higher product life can be achieved by setting A, B, C, D and E at their low levels and F and G at their high levels. Factor F was found to have the strongest effect.

If desired, further experiments can be conducted to study the interaction effects of these factors.

* Wu, Jeff and Hamada, Michael, Experiments: Planning, Analysis, And Parameter Design Optimization, John Wiley & Sons, New York, 2000.